## Slide 1: The basics of silicon detectors for radiation detection
J. Lee
Center for High Energy Physics
Kyungpook National University
3rd School for Particle Detectors and Applications
at KNU (SPDAK2022)
January 17, 2022
Notes: 경북대학교 고에너지 물리연구소 이직입니다. 실리콘검출기를 소개해드리겠습니다.

## Slide 2: Outline
Introduction
  Examples of silicon detectors
  Interaction of particles with silicon
Properties of silicon
Silicon detectors for charged particle detection
Silicon detectors for photon detection
Radiation damages in silicon detectors
Backgrounds in silicon detectors
Summary
They won’t be covered
due to the time constraint.
Notes: 제 발표 순서는 실리콘 검출기 종류, 하전입자 및 광자의 실리콘물질과의 상호작용으로 구성된 소개부분, 둘째 실리콘의 성질, 셋째 실리콘 하전입자 검출기, 넷째 실리콘 광센서, 마지막 Summary의 순서입니다.

## Slide 3: 1. Introduction

## Slide 4: Examples of Silicon Detectors for Charged Particle Detection
Pixel sensor for CMS
http://hep.fi.infn.it/CMS/sensors/Silicon_Detector.gif
Double-side strip sensor
Single-side strip sensor
Strip-pixel sensor

## Slide 5: Examples of Silicon Detectors for photon detections
8.4 mm
6.3 mm
Sony ICX493AQA APS-C, 6.05 μm pixel size, 10.14 M pixels, 23.4 mm × 15.6 mm, CCD from digital camera Sony α DSLR-A200 or DSLR-A300, sensor side
Samsung ISOCELL HM2 sensor, 0.7 μm pixel size, 12,000 × 9,000 (108 M) pixels, used in Xiaomi Redmi Note 9 Pro 5G and Xiaomi Mi 10i
Sensl SiPM pixel array, 8 × 8 pixels, 6 mm pixel size, 22,292 micro-pixels , 40 μm micro-pixel size
CCD
CMOS
SiPM

## Slide 6: Interaction of charged particles with silicon
By S. Banerjee
& A. Caner
Energy loss by ionization
We will not discuss about energy loss by radiation.
Note that for heavy particles.
Minimum Ionizing (Particles)
Relativistic rise
Eelectron ~ 0.7 MeV
when βγ=1
Mean dE/dx:
<dE/dx>

## Slide 7: Energy loss by ionization
3.6 eV required for producing a pair of e-h in Si
≈ 10,000 e-h pairs / 100 μm expected in Si
Bethe equation
z: charge of incident particle
<> ≈ 40 keV / 100 μm in Si for minimum ionizing particles
<> z2

## Slide 8: Interaction of photons with silicon
Photon energy (eV)
Photon energy (keV)
Photon energy (eV)
(A)
(B)
(C)
Compton
scattering
Photoelectric
effect
Pair production

## Slide 9: References for the plots in Page 8
Sze, S. M., Physics of Semiconductor Devices, John Wiley and Sons, N.Y., 1981; Jellison, Jr., G. E. and F. A. Modine, Appl. Phys. Lett- 41, 2 (1982) 180-182.
X-RAY DATA BOOKLET, Lawrence Berkeley National Laboratory
Durini (Editor), “High Performance Silicon Imaging: Fundamentals and Applications of CMOS and CCD Sensors”, Woodhead Publishing, 2014 Particularly: Chapter 10 (p286) by R. Turchetta, STFC, UK

## Slide 10: 2. Properties of silicon

## Slide 11: Band & bandgap
From ‘Semiconductor Devices
Physics and Technology Second Edition’
by S.M. Sze

## Slide 12: Indirect vs Direct Bandgap Semiconductors
Direct bandgap
Indirect bandgap
phonon
Si
GaAs
Excitation/De-excitation = Eg
Excitation/De-excitation = Eg + Ephonon
From ‘Semiconductor Devices
Physics and Technology
Second Edition’
by S.M. Sze

## Slide 13: Why Silicon?
abundant --> cheap
Lighter
SiO2 layer
  Naturally or inexpensively formed
  chemically and mechanically very stable
  effectively passivates the surface states of the underlying silicon
  forms an effective diffusion barrier for the commonly used dopant species
  easily preferentially etched from the silicon, and vice versa, with high selectivity
  By contrast, GeO2 is a chemically unstable, poor electrical insulator that is 33 times more soluble in water than SiO2, making it less suited to the photolithographic and wet chemical processes used to fabricate integrated circuits.

## Slide 14: Intrinsic Si semiconductor
low T : electrons bound in lattice
higher T : free electrons & holes
The crystalline structure is Diamond Cubic (FCC).
Bare wafers of <100> or <111> crystals are popular ones used for silicon detector fabrications.

## Slide 15: Impurities
Jargons

## Slide 16: Doping: acceptors & donors

## Slide 17: Effect of doping
Phosphorus-doped silicon

## Slide 18: 3. Silicon detectors for charged particle detection

## Slide 19: p-n junction (fundamental structure)
The depletion region d is a region
with no charge carriers (with no
free charges).
d
depletion depth

## Slide 20: p-n junction
depletion depth

## Slide 21: Depletion depth
d=
d=
d=
d=
d=
An exercise :
p-type Si
ρ ~ 10 kΩ cm
d ~ 300 μm
 V ~ 110 V
(V in Volts & ρ in Ω cm) for Si

## Slide 22: p-n junction reverse bias characteristics
I
I
C ∝Area/d
d = depletion depth

## Slide 23: PIN Diode
n
p
Intrinsic or
lightly doped
p
n
n+ p p+
In practice
n+ n p+
or
p-n junction
p-n junction
Ohmic contact
Ohmic contact

## Slide 24: When a charged particle traverses the depletion zone
~ 10,000 e-h pairs / 100 μm
Intrinsic or
lightly doped
Simple detector
n
p

## Slide 25: Silicon pixel sensor
PIN diode, DC type
Wafer: 5 inch, 525 μm in thickness, double polished side,
N-type high resistivity (>5 kΩ-cm), (111) orientation
pixel size = 1.55 cm x 1.38 cm
variable
4x4 pixels

## Slide 26: C-V measurement for a single pixel
1/C2
1/C2
1/C2
V
1/C2
V
C
C in 10-11 F
1/C2 in 1020 F-2
C ∝Area/d

## Slide 27: I-V measurement for a single pixel
V
I(nA)
I
I
The deviation from the expected is
due to the surface current.
Still 5nA @ 200V is excellent.
?

## Slide 28: dE/dx is of random nature: if Gaussian distribution
dEp/dx = <dE/dx>
dE/dx
dE
thickness: x 2x 4x
σ σ σ
5
σ
5
most probable dE = dEp
mean dE/dx

## Slide 29: dE/dx is of random nature: Landau Distribution
Due to δ rays:
Knock-on electrons
dEp
Simulation of Energy loss in silicon: 100 GeV Proton, 380 μm thickness
wFWHM = 4.02
λ = - -1+)
<dE>
=

## Slide 30: dE/dx is of random nature: if Landau distribution
σ 2σ 4σ
5 >>
σ σ σ
5 >5 >5
dEp ∝ x[a+ln(x)]
thickness: x 2x 4x
dEp /dx
11.7 12.0 12.3
dE
dE/dx
<dE/dx>
What will happen as x gets large?

## Slide 31: dE/dx is of random nature: if Gaussian convoluted Landau distribution
dE (keV)
dE/dx (keV/μm)
S. Meroli, 2011 JINST 6 P06013

## Slide 32: dE/dx is of random nature: if Hans Bichsel’s Straggling function
From Review of Particle Physics

## Slide 33: 90Sr source test for a single pixel
trigger
pixel
the pixel
of interest
electrons
Change the bias voltage of the pixel
CERN Note
PH-EP-Tech-Note-2015-003
Electron Energy is NOT mono-energetic !

## Slide 34: Signal as a function of bias voltage
Vbias = 21V, Vbias = 60V, Vbias = 167V
pedestal
ADC
Signals fitted with Gaussians.
Use these fit results !
pedestal
ADC
Signals fitted with Landau functions.
Not very good fits!

## Slide 35: Depletion depth vs. bias voltage
V
d ∝ Peaksignal – Peakped (ADC)
120 V

## Slide 36: wdE/dx vs.
120 V
1/x form expected !

## Slide 37: Pedestal width vs. bias voltage
Vbias = 167V
Vbias = 0V
Why σped @ OV >> σped @ 167V?
ADC
Practically Useful! How?

## Slide 38: Silicon Pixel Sensor & Ladder for SCD
pixel size = 1.55 x 1.38 cm2
Built by SKKU group
4x4 pixels
One sensor

## Slide 39: Heavy Ion Beam Test of 4-layer prototype @ CERN

## Slide 40: Prototype Performance: Response to Heavy Ions
single-layer A1
2-layer
(A1+A2)/2
3-layer average
(A1+A2+A3)/3
4-layer average
(A1+A2+A3+A4)/4
Histogram = SCD response = ADC = dE/dx ∝ Z2
Curve = Best Fit to Histogram
δ(dE/dx) ↓
as # of layer ↑
Ai =ADC(ith layer)

## Slide 41: Prototype Performance: Charge Resolution of Fe as a func. of layer
δZ4L = (1.16 0.07) 10-1
δZ3L = (1.39 0.10) 10-1
δZ2L = (1.65 0.10) 10-1
Z
2-layer
(Z1+Z2)/2
3-layer average
(Z1+Z2+Z3)/3
4-layer average
(Z1+Z2+Z3+Z4)/4
δZ ↓ as # of layer ↑
δZ4L = δZ2L /
0.116 ≈ 0.117
δZ3L = δZ2L
0.139 ≈ 0.135

## Slide 42: Silicon Charge Detector (design, fabrication & assembly
Built by SKKU group

## Slide 43: Silicon Charge Detector (specification)

## Slide 44: ISS-CREAM payload
BSD
Instrument
BCD
Instrument
TCD
Instrument
Calorimeter
PIU
Electronics
Rack (1 of 3)
Grapple Fixture
(1 of 2)
Calorimeter
Composite Base
Plate
Targets
HPDs
(2 of 4)
Power
Distribution
Boxes
ATCS
BSD
Electronics
Readout Box
Fluid Loop
Accumulators
Not Shown (Located behind Power Distribution Boxes
Housekeeping Box
Science Flight Computers
Vents
(1 of 2)
4-layer SCD
(built by SKKU group)
Mass ~ 1258 kg
Power ~ 415 W
Length ~ 185 cm

## Slide 45: ISS-CREAM @ GSFC before TVAC test (July 22-25, 2015)

## Slide 46: ISS-CREAM in space operation

## Slide 47: SCD performance: standalone tracking
θ = 34.19 +1.91 -0.59°
φ = 105.5 +5.9 -2.9°
layer1
layer2
layer3
layer4
A 4-layer track!

## Slide 48: SCD performance: charge measurement
Very early data!
C
N
O
Ne
Mg
Si
S
Fe
z

## Slide 49: 4. Silicon detectors for photon detection

## Slide 50: CCD (Charge Coupled Device) sensor
Charge Coupled Device
Photoelectrons produced by photoelectric effect

## Slide 51: CCD analogy
output = charge

## Slide 52: CCD inventors (winners of Nobel prize in physics in 2010)
Having Fun @ Bell Lab in 1974 !
G. E. Smith & W.S. Boyle : invented CCD in 1970

## Slide 53: CCD application in Astronomy/Astrophysics

## Slide 54: CMOS sensor
PD = Photo Diode
output = voltage
CMOS : Complementary Metal Oxide Semiconductor
Notes: PD는 수광부인 photodiode이고, TG는 전하를 전달하는 Transmission Gate입니다, 전달된 전하는 FD 즉 Floating Diffusion에서 전압으로 변환됩니다.
SF =source follower = Buffer, SEL = line selection, RS= Reset

## Slide 55: A pixel in CMOS sensor
Amplifier converts charge signal to voltage signal !

## Slide 56: Layout of typical CMOS sensor

## Slide 57: CCD & CMOS summary
  원칙적으로는 동일, 즉 포토다이오드 구조로, 광의 세기가 전하량으로 변환되고, 전하를 전압으로 변환 출력
  변환기가 어디에 위치하는가가 두 센서의 근본적인 차이
  픽셀의 정보 이동 방법의 차이, 즉 CCD는 전하로 픽셀간 이동 최종 전압으로 변환, CMOS는 픽셀 단위에서 전압으로 변환하여 이동
  잡음이 크고, 동적폭 (dynamic range) 및 속도에서 뛰어나지 않음
  동적폭 = Full Well Capacity / 잡음
  Kodak Mega 픽셀 CCD: 200,000 전자 / 20전자 = 100,000
  광량이 적은 환경에서는 고민감도의 센서가 필요하나, CCD와 CMOS는 증폭형 센서가 아니므로 어두운 상황에서 그 성능에 한계
  우리의 눈의 민감도는 CCD 보다 우수함
  CCD 민감도 ~ 0.03 Lux (냉각 시 0.002 Lux)

## Slide 58: Photomultiplier
정확히 말하면 광전자를 다수의 전자로 증폭
광음극(photocathode)과 함께 사용하는 PMT(Photomultiplier Tube) 와 MCP(Microchannel Plate)가 대표적으로 단일 광자 계수 가능
반도체 소자에서는 센서 내부에서 광전자(photoelectron)를 증폭: ICCD(Intensified CCD), EB(Electron Bombardment)CCD, EM(Electron Multiplier)CCD, APD(Avalanche Photodiode), SiPM(Silicon Photomultiplier)

## Slide 59: Photomultiplier Tubes (PMTs)
초민감 초고속 특성을 갖는 광센서로 과거 수십년간 특수목적에 사용
그러나 진공관식으로 부피가 매우 크고, 충격에 취약하며 고전압을 필요로 하므로, 내구성, 휴대성 및 실용성이 크게 떨어지며, 광량이 많아지면 소자가 파괴되는 문제
PMT의 원리와 Hamamatsu사 제품

## Slide 60: 20 inch World largest PMT
For Super-K

## Slide 61: SiPM
Single micro-pixel
Micro-pixel: Avalanche Photo Diode (APD) in Geiger mode
  Size of micro-pixel = tens of μm
  Gain ≥ 106
  Distinctive binary single photo-electron signal
Micro-pixels in a SiPM are connected through quenching resistors (RQ) to a common output.
SiPM: 1000 – 10000 micro-pixels / 1 mm2
SiPM output: Sum of binary signals (Analog)
--> counts the incident photons
From Hamamatsu SiPM handbook

## Slide 62: Geiger Mode

## Slide 63: SiPM
PN 접합면에 매우 높은 전기장 형성
한 개의 광자 입사 -> 100만 배의 전자증폭 발생 -> 초 민 감 도 !!
광이 입사되었을 때 센서의 반응 속도 -> 1ns 초 고 속 도 !!
2
1
N+
P+
Electric field
106
102
104
0
E (V/cm)
X (um)
3
4
5
6
SiPM의 Micropixel

## Slide 64: Analog Signal
e
Q = nQ1 ?
e
ne
single
micro-pixel

## Slide 65: Photon Counting Capability
Waveform
Charge distribution

## Slide 66: 다화소용 8 x 8 픽셀 어레이 소자
SiPM 픽셀
  : 1 x 1 mm2 크기
  (30x30μm2크기, 103개의 마이크로 픽셀)
64ch SiPM 소자 : 1 x 1 cm2
1cm
1cm
1
1
64ch 설계도
64ch SiPM 센서(1cm2)의 현미경 사진
1cm
1cm
1
2
3
4
5
6
7
8
2
3
4
5
6
7
8

## Slide 67: 1024 화소 배열
1024 화소 구성
단위소자
= 8x8 화소
1024 화소
= 4x4 단위소자
화소
1mm x 1mm
8mm x 8mm
32mm x 32mm
30μm
30μm
32x32 = 1024
mircro-pixels
in parallel
a micro-pixel

## Slide 68: 16개의 8 x 8 SiPM 픽셀 어레이로 구성된 다화소 (1024-ch)
항복전압 균일
->
Multi channel test
4cm
4cm
1단계 SiPM 픽셀 1024ch 제작
  : 1 x 1 mm2 크기
  (30x30μm2크기, 103개의 마이크로 픽셀)
64ch SiPM 소자 : 1 x 1 cm2
1024-ch
Voltage(V)

## Slide 69: 1024-ch SiPM + 신호처리장치 + Pinhole
Pinhole
Electronics

## Slide 70: Image Test
SiPM
Pinhole
10 cm
10 cm
A
A
Pinhole Camera

## Slide 71: Image Test
Pinhole Camera
200 cm
Absolutely Dark!
CCD or CMOS cameras
can NOT get this image!

## Slide 72: 5. Radiation Damages in silicon detectors

## Slide 73: Bulk damage
Displacement of lattice atoms
Defects can be active with levels in the band gap
  capture and release electrons and holes from conduction and valence bands
  trapping centers, generation/recombination centers,
Particles
Distributions
of vacancies in μm3
after 1014 particles/cm2
NIMA 491 (2002) 194
Mainly clusters

## Slide 74: Surface damage
Qit: holes trapped in the interface
Microelectronic Technology Thermal Oxidation (III)
by Bhargav Veepuri
Si-SiO2 interface
Radiation produces e-h pairs in SiO2.
Some of these charge carriers recombine.
Some carriers move to the electrodes.
Some holes (with lower mobility) drift to be fixed oxide charges near the Si-SiO2 interface.
Some holes drift to the Si-SiO2 interface to be interface traps.

## Slide 75: Radiation damages: two types
Bulk (Crystal) damage due to Non Ionizing Energy Loss (NIEL): Displacement Damage
  Increase of leakage current (increase of noise)
  Change of depletion voltage (higher operation voltage, under-depletion)
  Decrease of charge collection efficiency due to under-depletion and increased trapping
Surface damage due to Ionizing Energy Loss (IEL): Accumulation of positive in the oxide (SiO ) and the Si/SiO2 interface
  Increase of leakage current with breakdown behavior
  Change of depletion voltage (higher operation voltage, under-depletion)
  Increase of inter-pixel capacitance (noise factor) & decrease of inter-pixel resistance
  Formation of an electron accumulation layer, which may cause charge losses at the interface.

## Slide 76: 6. Backgrounds in silicon detectors

## Slide 77: Leakage current or Dark current in silicon
Free charge carriers can also be generated in absence of signal(charged particles or photons) by thermal excitation or tunneling and produce an avalanche breakdown:
Direct thermal transition
Trap-assisted thermal transition
Direct tunneling effect
Trap-assisted tunneling effect
M. Nitschke-michael Master’s degree, Universität Hamburg, 2016

## Slide 78: Optical Cross-Talks Background in SiPM
Manifestation of Optical Cross-Talks
From Hamamatsu SiPM handbook

## Slide 79: Manifestation of After-Pulses in SiPM
During an avalanche process (whether triggered by a photoelectron or a thermal carrier), a small portion of avalanching carriers get trapped in impurity energy levels but are released after short delays (typically on the order of few 10 ns) upon receiving the required energy (albeit small) to reenter the conduction or valence band.
Upon their release, these carriers initiate new avalanche pulses, which appear with delays after the genuine parent pulse and are hence referred to as after-pulses.
From Hamamatsu SiPM handbook

## Slide 80: Manifestation of After-Pulses in SiPM
During an avalanche process (whether triggered by a photoelectron or a thermal carrier), a small portion of avalanching carriers get trapped in impurity energy levels but are released after short delays (typically on the order of few 10 ns) upon receiving the required energy (albeit small) to reenter the conduction or valence band.
Upon their release, these carriers initiate new avalanche pulses, which appear with delays after the genuine parent pulse and are hence referred to as after-pulses.
From Hamamatsu SiPM handbook

## Slide 81: 5. Summary

## Slide 82: Summary
Silicon is one of most popular material for radiation detection in the fields of Particle physics/Astro-particle physics
  Charged particle detection, Photon detection, etc.
Examples are given to help the audience understand
  C-V & I-V characteristics of silicon detectors
  Responses (signals) of silicon detector to charged particles
    dE/dx as a func. of Vbias
    dE/dx as a func. of the number of measurements (layers)

## Slide 83: Back-up slides

## Slide 84: Sand to silicon wafer

## Slide 85: Recipe for fabrication process
Clean wafer
Oxidation
Cover with photoresist
Expose through mask
Develop
Etch SiO2
N+Diffusion
P+ Implantation Anneal
Metallization

## Slide 86: Example of CMOS fabrication process
From
https://en.wikipedia.org/wiki/CMOS

## Slide 87: Absorption Coefficient
From ‘Semiconductor Devices
Physics and Technology Second Edition’
by S.M. Sze