## Slide 1
Research and Development of Ultrawide-Band Ultraviolet Laser Using Cerium-Doped Fluoride Crystal
CHEP Joint International Workshop: Detector Development for High Energy Physics and Various Applications &
7th Luminescence Materials Workshop
High-1 Resort @ Jeongseon, Korea
12 ~ 13 Feb. 2025
PHAM HONG MINH
Institute of Physics, Vietnam Academy of Science and Technology

## Slide 2: BRIEF INTRODUCTION TO IOP
IOP is the first institute of VAST, established in 1969
Notes: Research institutes with the same function are merged.

## Slide 3
IOP NEW BUILDING

## Slide 4
BRIEF INTRODUCTION TO CQE
Centre for Quantum and Electronics
Photonics
Laser spectroscopy
Nano-bio photonics

## Slide 5
DIODE-PUMPED PS SOLID - STATE LASER
NOVEL MATERIALS FOR LASER APPLICATIONS
LASER SPECTROSCOPY AND APPLICATIONS
ALL SOLID – STATE ULTRAVIOLET
LASERS
ALL SOLID STATE RAMAN LASER
ALL SOLID STATE
HIGH POWER ULTRASHORT LASER
RESEARCH AND DEVELOPMENT OF ALL SOLID-STATE LASERS AT PHOTONIC LABORATORY
Notes: Currently, the Vietnamese government is focusing on investing in research on new materials for military applications.

## Slide 6
Femtosecond tunable dye laser
RESEARCH AND DEVELOPMENT OF ULTRA-SHORT ALL SOLID-STATE LASERS AT PHOTONIC LABORATORY

## Slide 7
Generation of picodecond laser pulses at 1064
from all solid state passively mode-locked Nd3+:YVO4 lasser
Resonator configuration of the diode end pumped passively mode-locked Nd:YVO4 laser
RESEARCH AND DEVELOPMENT OF ULTRA-SHORT ALL SOLID-STATE LASERS AT PHOTONIC LABORATORY
Notes: We s

## Slide 8
DIODE-PUMPED PICOSECOND Nd3+:YVO4 LASER

## Slide 9
τ  20 ps
H×nh 3.6: VÕt tù t­¬ng quan thu ®­îc b»ng hÖ ®o autocorrelator.
Autocorrelation trace of passively mode-locked Nd:YVO4 laser pulse corresponding to a pulse duration of 12 ps
Gauss fit
Power characteristics of passively mode-locked Nd:YVO4 laser
Spatial intensity distribution
Pulse trains of passively mode-locked Nd:YVO4 laser
Output power (mW)
Pump power (mW)
DIODE-PUMPED PICOSECOND Nd3+:YVO4 LASER

## Slide 10
DIODE-PUMPED PICOSECOND Nd3+:YVO4
COMPACT LASER

## Slide 12
HIGH POWER ULTRASHORT ALL SOLID STATE LASER

## Slide 13
M1
M3
M2
G1
M9
M4
D_Gr1
Ti:sp
M7
M6
M5
M13
M11
M12
M8
M10
L1
L2
M14
M15
M20
M16
M17
M19
D_Gr1
M18
M21
M22
/2
L4
L3
L5
PP
FS LASER AMPLIFIER

## Slide 14
Pulse energy: 800 J (10 nJ seed)
Pulse duration: <150 fs
Repetition rate: 10 Hz
Wavelength: 800 nm

## Slide 15
APPLICATION OF FS LASER AMPLIFIED
Development of a power amplifier for ultrashort laser pulse with pulse duration less than 100 fs and pulse energy up to 800 μJ.
Research and apply amplified laser in ultrafast spectroscopy for subjects of biomedical and materials science.
Research and laser applications in ultrafast spectroscopy for subjects of biomedical and materials science.

## Slide 16: LASER APPLICATIONS
Spectroscopy
Optical lithography
Material assessment
Laser processing
L. Skuja et al., J. Non-Cryst. Solids 353, 526 (2007).
T. Suganuma et al., Opt. Lett. 27, 46 (2002).
S. Park et al., J. Vac. Sci. Tech. 20, 2108 (2002).
R. H. French et al., Aust. J. Chem. 60, 251 (2007).
S. T. Park et al., Nature 415, 306 (2002).
S. W. J. Scully et al., J. Phys. B:At. Mol. Opt. Phys. 35, 2703 (2002).
P. R. Herman et al., Appl. Surf. Sci. 154-155, 577 (2000).
The advancement of these applications highly depend on the investigations of UV light sources and the improvement of their optical properties
Notes: My main research field is the development of laser and amplifier systems for example Diode-pumped ps and fs solid-state lasers, All solid-state ultraviolet lasers, All solid-state Raman lasers and In recent years I also focus on research on new laser materials.
The ultraviolet (UV) laser has received a great deal of interest for numerous applications in many fields of science and technology. The most established applications include environmental sensing, engine combustion diagnostics, semiconductor processing, optical micro machining, optical communications, medicine and biology [1-4]. The advancement of these applications highly depend on the investigations of UV light sources and the improvement of their optical properties. Therefore, the improvement of laser materials or laser quality in this wavelength region is very important.

## Slide 17
B Napier et al, Ultra-broadband infrared gas sensor for pollution detection: the TRIAGE project, Journal of Physics: Photonics, Vol 3, 2021, pp. 031003(1 - 7).
APPLICATION OF LASER
Ultra-broadband infrared gas sensor for pollution detection
Notes: As you know, the air is increasingly polluted due to many factories.

## Slide 18
Absorption spectrum of SO2
APPLICATION OF LASER
Ultra-broadband infrared gas sensor for pollution detection
Pollutant gases play an important role in influencing air quality. Hence, assessment of the concentration and distribution of these gases in the atmosphere is important. Some gases, particularly sulfur dioxide (SO2) and ozone (O3) strongly absorb UV radiation.
B Napier et al, Ultra-broadband infrared gas sensor for pollution detection: the TRIAGE project, Journal of Physics: Photonics, Vol 3, 2021, pp. 031003 (1 - 7).
Notes: Monitoring these gases using DIAL requires a tunable laser system that simultaneously emits two wavelengths, each with a spectrally narrow linewidth. Whereas a linewidth of 1 nm is enough for detecting O3, this is too wide for detecting SO2. Due to the low concentration and low absorption cross section of SO2, more than two lines within its absorption wavelength range are needed for accurate measurement. Hence, a linewidth that is smaller than 100 pm is required

## Slide 19
LASER PARAMETERS
Energy
Pulse duration
Wavelength

## Slide 20
UV LASERS AND THEIR APPLICATIONS
There are various kinds of lasers which can generate ultraviolet
Its complexity, high cost, limited spectral bandwidth and tunability, inefficiency, inconvenience and unreliability.
Notes: Primarily, the existing commercially available tunable UV laser sources, comprising of subsequent steps of nonlinear frequency conversion such as doubling, tripling, and/or mixing of tunable radiation obtained from traditional tunable visible or near infrared lasers have been difficult to use. The main disadvantages of such devices are their complexity, high cost, spectral bandwidth and tunability limitation in accordance with experimental requirements
There are various kinds of lasers which can directly generate ultraviolet
Excimer lasers are very powerful UV sources, also emitting nanosecond pulses, but with average output powers between a few watts and hundreds of watts. Typical wavelengths are between 157 nm (F2) and 351 nm (XeF).

## Slide 21
Aspect | Properties
important types | XeF lasers for 351 nm; ArF lasersfor 193 nm; F2 lasers for 157 nm
Applications | UV lithography; laser ablation andpulsed laser deposition; lasermarking;eye surgery; pumping dyelasers
Pump source | electrical current
Power efficiency | 0.2% to 2%
Accessible wavelengths | various lines in the ultraviolet region
Wavelength tuning | quite limited
Average output power | typically between 10 W and 300 W
Beam quality | sometimes close to diffraction-limited; sometimes worse
Continuous-wave operation | no
Nanosecond pulse generation | always (pulsed pumping)
Picosecond & femtosecond pulse generation | no
PROPERTIES OF EXCIMER LASERS

## Slide 22
DEVELOPMENT OF ULTRAVIOLET LASER
UV laser based on frequency conversion using nonlinear crystals such as doubling, tripling and/or mixing of tunable laser emission generated from the primary tunable lasers
Karl F. Renk, Basics of Laser Physics For Students of Science and Engineering, (2017)
Walter Koechner, Solid-State Laser Engineering, Springer Science, ISBN-10: 0-387-29094-X, (2006).
Notes: For the UV laser based on frequency conversion using nonlinear crystals such as doubling, tripling and/or mixing of tunable laser emission generated from the primary tunable lasers. However, this way has several disadvantages such as its complexity, high cost, limited spectral bandwidth and tunability, inefficiency, inconvenience and unreliability for airborne measurement in flight or aboard spacecraft applications
exity, high cost, spectral bandwidth and tunability limitation in accordance with experimental requirements

## Slide 23
Laser emission | Wavelength (nm) | Pulse energy
DFDL | 565,8 | 0,62 mJ
 | 572,8 | 1,8 mJ
UV | 282,9 | 30 J
 | 286,4 | 60 J
UV LASER BASED ON FREQUENCY CONVERSION

## Slide 24
5 Ce3+ ion doped fluoride crystals are reported
KrF laser
pumping
(248 nm)
(1979)
Wavelength (nm)
250 300 350
Ce
3+
:YLiF
4
(305-335 nm)
Ce
3+
:LaF
3
(275-315 nm)
Ce
3+
:LuLiF
4
(305-335 nm)
Ce
3+
:LiSrAlF
6
(280-325 nm)
4
w
of Nd:YAG
laser pumping
(266 nm)
Ce
3+
:LiCaAlF
6
(280-325 nm)
5
w
of Nd:YAG
laser pumping
(213 nm)
(1994)
(1993)
(1992)
(1980)
+ 266-nm pump possible
Ce:LiCAF, Ce:LiSAF
+ No degradation
for Ce:LiCAF
– Ce:LiSAF, Ce:YLF
Solarization reported
1
2
4
3
5
1. P. F. Moulton, et. al, OL4, 184 (1979)
2. P. F. Moulton ,et. al, OL5, 339 (1980)
3. M.A. Dubinskii, et. al, IQEC1992. FrL2
4. M.A. Dubinskii, et. al, JMO. 40, 1, (1993)
5. C.D. Marshall, et. al, JOSAB. 11, 2054 (1994)
All Ce doped have abroad gain band width. They are especially attractive for ultrashort-pulse generation and application.
DEVELOPMENT OF ULTRAVIOLET LASER
Notes: In this regard, high-power, all-solid-state UV lasers based on rare earth-doped fluoride crystals are still highly regarded, Among possible UV materials,
fluoride crystals have been developed for the direct and efficient generation of UV light. One of the fluoride crystals is cerium-LiCAF

## Slide 25
Fluoride crystals have been developed for the direct and efficient generation of UV
Laser medium
Broad band: 280 to 325 nm
Tunable, high-energy, short-pulse, all-solid-state laser
Ce:LiCaAlF6（Ce:LiCAF）
Availability in large, high-quality crystals
Pumped using the 4ω (266 nm) of Nd:YAG laser
Good conversion efficiency
Broad gain bandwidth
High effective gain cross-section: 6 × 10-18 cm2
Large saturation fluence: 115 mJ/cm2
Fluorescence lifetime: 30 ns
Absorption and luminescence spectrum
DEVELOPMENT OF ULTRAVIOLET LASER
Notes: Ce3+-doped LiCaAlF6 (Ce:LiCAF) is an especially attractive solid-state laser gain medium for all-solid-state laser generation and short-pulse amplification in the UV region.
Focusing on its laser applications, Ce:LiCAF offers several advantages compared to other laser materials. Aside from being grown into large, high-quality crystals, Ce:LiCAF can be pumped using the fourth harmonics of an Nd:YAG laser and demonstrates good conversion efficiency.
It also has a broad gain bandwidth and a high effective gain cross-section (as shown here) useful in UV short pulse generation and high-power laser amplification.
In addition,
Ce:LiCAF has large saturation fluence
and 30-ns fluorescence lifetime
which are all necessary for multi-pass amplifier systems.
Because Ce:LiCAF has a strong absorption at 266 nm, the fourth harmonic (4th harmonic) of the Nd:YAG laser is an ideal pump source.
Ce:LiCAF has a potential tuning range from 280 to 320 nm [7]. This tuning range is attractive for short pulse applications.
Ce:LiCAF has a sufficiently higher effective gain cross-section (6x10-18 cm2) compared with Ti:sapphire [14]. This property makes it favorable for designing laser oscillators.
Ce:LiCAF has a larger saturation fluence (115 mJ/cm2) than organic dyes [8]. This makes it attractive for designing power amplifiers.
The fluorescence lifetime of Ce:LiCAF was reported to be 30 ns and is shown in Figure. 2.4 [15]. This lifetime is shorter than that of Ti:sapphire. Although it is too short for constructing regenerative amplifiers, it is long enough for designing multipass amplifiers and also long enough for electric delay control of the amplifier timing.
The ﬂuorescence lifetime of Ce:LiCAF was reported to be 25 ns. It would be too short for constructing regenerative ampliﬁer; it is long enough for designing multi-pass ampliﬁers and also long enough for electronic delay control of the ampliﬁer timing.

## Slide 26
P=120 mW; α =19 0 – 230;
0,6 nm
TUNABLE ULTRAVIOLET LASER
Wavelength Tuning: 280 - 298 nm
Thời gian (nm)
3.5 nm
Output power (mW)
Pump power (mW)
Time (ns)
Wavelength (nm)
0.2 (nm)
Wavelength (nm)
Wavelength (nm)
Wavelength (nm)
Wavelength (nm)
Notes: Góc quay của cách tử so với trục của BCH ~ 20,30, (288.5 nm), L=6.5 cm; R=30%; Rg=30%
ngưỡng phát laser được xác định tại công suất bơm ~ 40 mW;
Năng lượng laser bơm được giữ không đổi là ~120 mW (~3 lần trên ngưỡng). 19 0 đến 230, vùng điều chỉnh bước sóng đạt được là 11 nm từ 285 nm đến 296 nm

## Slide 27
Pham Van Duong, Pham Hong Minh et al, Development of short pulse broadband and tunable narrow-linewidth ultraviolet laser lasers using Ce:LiCAF crystal, Communications in Physics, Vol. 29, 2019, pp. 341- 349.
BROADBAND ULTRAVIOLET LASER

## Slide 28
Experimental and theoretical spectral profiles of the 288.5-nm seed pulses after amplification.
Output energy and gain after each round trip in the 4- pass amplifier. Black data points refer to experimentally measured data while red data points refer to calculation results
DYNAMICS OF MULTI PASS AMPLIFIER USING Ce:LiCAF CRYSTAL

## Slide 29
Diep Van Nguyen, Minh Hong Pham et al, Theoretical and experimental study of ultraviolet broadband laser amplification using CeLiCAF crystal. Optics Communications, Vol. 530, 2023, pp.129165(1 - 10).
BROADBAND ULTRAVIOLET LASER

## Slide 30
DYNAMICS OF MULTI PASS AMPLIFIER USING Ce:LiCAF CRYSTAL

## Slide 31
HOW TO REACH ULTRAWIDE –BAND ULTRAVIOLET LASER
Supercontinuum generation
Modeless laser

## Slide 32
Callum R. Smith, Ole Bang et al, Low‑noise tunable deep‑ultraviolet
supercontinuum laser. Scientific Reports, Vol. 10, 2020, pp.18447(1 - 11).
Low‑noise tunable deep‑ultraviolet supercontinuum laser.
SUPERCONTINUUM GENERATION
Notes: anti‑resonant hollow‑core (AR HC) fiber - sợi lõi rỗng chống cộng hưởng (AR HC)
Thiết lập thử nghiệm: L1, L2, L3 = thấu kính phẳng lồi silica hợp nhất UV phủ chống phản xạ, L4 = thấu kính phẳng lồi canxi florua không phủ, W1 = cửa sổ mặt phẳng silica hợp nhất UV phủ chống phản xạ, W2 = cửa sổ mặt phẳng canxi florua không phủ, DM = gương tán sắc, OAP = gương parabol lệch trục nhôm tăng cường UV, BPF = bộ lọc thông dải phổ.
resonant dispersive wave RDW - sóng phân tán cộng hưởng RDW
Bước sóng trung tâm củaRDW có thể được điều chỉnh giữa 236 và 377 nm bằng cách điều chỉnh áp suất Ar trong sợi dài 140 mm

## Slide 33
Callum R. Smith, Ole Bang et al, Low‑noise tunable deep‑ultraviolet supercontinuum laser. Scientific Reports, Vol. 10, 2020, pp.18447(1 - 11).
Low‑noise tunable deep‑ultraviolet supercontinuum laser.
SUPERCONTINUUM GENERATION
Notes: Thiết lập thử nghiệm: L1, L2, L3 = thấu kính phẳng lồi silica hợp nhất UV phủ chống phản xạ, L4 = thấu kính phẳng lồi canxi florua không phủ, W1 = cửa sổ mặt phẳng silica hợp nhất UV phủ chống phản xạ, W2 = cửa sổ mặt phẳng canxi florua không phủ, DM = gương tán sắc, OAP = gương parabol lệch trục nhôm tăng cường UV, BPF = bộ lọc thông dải phổ.
resonant dispersive wave RDW - sóng phân tán cộng hưởng RDW
Bước sóng trung tâm củaRDW có thể được điều chỉnh giữa 236 và 377 nm bằng cách điều chỉnh áp suất Ar trong sợi dài 140 mm

## Slide 34
SUPERCONTINUUM GENERATION
AT IOP

## Slide 35
SUPERCONTINUUM GENERATION IN HEAVY METAL OXIDE SOLID CORE PHOTONIC CRYSTAL FIBERS
Wavelength (nm)

## Slide 36
Michael Soo, Nick Glumac, Ultraviolet absorption spectroscopy in optically dense fireballs using broadband second-harmonic generation of a pulsed modeless dye laser. Applied Spectroscopy, Vol. 68, 2014, pp. 517 – 24.
Laser dye modeless.
MODELESS ULTRAVIOLET LASER
Notes: To increase the sensitivity of the analysis, as well as the accuracy, the laser energy is increased.

## Slide 37
Michael Soo, Nick Glumac, Ultraviolet absorption spectroscopy in optically dense fireballs using broadband second-harmonic generation of a pulsed modeless dye laser. Applied Spectroscopy, Vol. 68, 2014, pp. 517 – 24.
MODELESS ULTRAVIOLET LASER
Notes: Một trong những phương pháp phát bức xạ laser phổ siêu rộng (modeless laser) đó là phương pháp khuếch đại toàn miền phổ phát xạ của môi trường hoạt chất. Phương pháp này đã được ứng dụng chủ yếu cho các laser màu.

## Slide 38
(5)
(6)
.
1 — MgF2–TiO2–SiO2–TiO2,
2 — MgF2–2[TiO2–SiO2]–TiO2,
3 — MgF2–3[TiO2–SiO2]–TiO2,
4 — MgF2–4[TiO2–SiO2]–TiO2
M. H. Maleki, S. Batebi et al, Design and Fabrication of fabrication of variable reflectivity mirrors with Gaussian profile for Nd:YAG lasers, Journal of Applied Spectroscopy, Vol. 80, 2013, pp. 615–619.
S. De Silvestri, Valentini et al, Q-switched Nd:YAG laser with super-Gaussian resonators, Optics Letters, Vol. 16, 1991, pp. 642-644.
ULTRAWIDE -BAND ULTRAVIOLET LASER

## Slide 39
(7)
Wavelength (nm)
Wavelength (nm)
Reflection coefficient
Reflection coefficient
Dependence of the mirror reflection coefficient at the different wavelengths
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER

## Slide 40
N=N0+N1
β = -ln(R1R2)
Diep Van Nguyen, Minh Hong Pham et al, Optics Communications, Vol. 496, 2021, pp. 127131.
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Notes: Với nhiều ưu điểm vượt trội, môi trường tinh thể Ce:LiCAF đã thu hút được nhiều nhóm nghiên cứu trên thế giới như: Viện nghiên cứu Vật liệu thuộc Đại học Tohoku, Nhật Bản nghiên cứu phát triển các tinh thể Ce:LiCAF [23, 24]; trường đại học Osaka, Nhật Bản phát triển các nguồn laser công suất cao, điều chỉnh bước sóng [14 -19]; Đại học Macquarie Sydney, Úc phát triển các nguồn laser điều chỉnh bước sóng và laser xung cực ngắn [25, 26]; Trung tâm nghiên cứu NASA Langley của Mỹ ứng dụng các nguồn laser tử ngoại băng hẹp Ce:LiCAF vào kĩ thuật Lidar nghiên cứu khí quyển [27]

## Slide 41
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Intensity (a.u. )
Wavelength (nm)

## Slide 42
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Wavelength (nm)
Intensity (a.u. )

## Slide 43
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Wavelength (nm)
Intensity (a.u. )

## Slide 44
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Laser configuration

## Slide 45
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Laser configuration

## Slide 46
RESEARCH AND DEVELOPMENT OF ULTRAWIDE -BAND ULTRAVIOLET LASER
Wavelength (nm)
Wavelength (nm)
Output power: 8 mW
These research findings open many potential applications for ultrawide-band ultraviolet lasers for environmental research
Intensity (a. u.)
Intensity (a. u.)
Notes: Khi được khuếch đại, hiệu ứng thu hẹp phổ xẩy ra, phổ sau khuếch đại co hẹp lại về dãy bước sóng từ 275 nm đến 335 nm, đồng thời đỉnh phổ được nâng lên, đỉnh phát xạ dịch chuyển ít về phía bước sóng dài ở khoảng gần bước sóng 290 nm

## Slide 47
Differential absorption spectroscopy DOAS schematic diagram
DEVELOPMENT OF DIFFERENTIAL ABSORPTION SPECTROSCOPY (DOAS) USING UV LASER
Notes: Before developing the DOAS system and researching gases in the atmosphere, it is necessary to evaluate the performance of DOAS at a laboratory scale. Therefore, the DOAS using Ce:LiCAF laser has been developed, the DOAS schematic diagram and experimental system shown in Figure 4. The structure of the DOAS can be divided into three main parts, namely: (1) excitation laser, (2) air chambers, and (3) signal reception and data processing system.
Excitation laser: The laser system has been developed and reported in section 2. To increase the absorption of SO2 gas, the laser beam will be guided through the chambers twice by aluminum-plated mirrors R1 and R2 with a high reflection coefficient of over 90 % in the wavelength range 280 to 320 nm.
Air chambers: The air chambers have a length of 0.5 m and diameter 0.06 m. Two windows made of quartz allow UV radiation to pass through. Two pump valves (S1, S2) and two exhaust valves (S3, S4) are responsible for continuously pumping and releasing gas in the chambers.
Signal reception and data processing system: Laser signals via fiber optic cable are guided to a spectrometer (Avaspec-HSC 1024 𝑥 58TEC-EVO) with an operating wavelength range from 200 nm to 385 nm and a resolution of 0.6 nm.

## Slide 48
DEVELOPMENT OF DIFFERENTIAL ABSORPTION SPECTROSCOPY (DOAS) USING UV LASER
Experimental system for measuring actual SO2 gas concentration
The standard SO2 gas (100 ppm ±2% was introduced into the chamber. The gas flow rate is kept constant at 3 L/min to maintain the gas concentration at 100 ppm.
The spectral characteristics of the Ce:LiCAF laser when passing through the air chamber will be recorded by the spectrometer two times. The first time, no SO2 gas and the second time, the air chamber is filled with SO2 gas.
The results of measuring standard SO2 gas concentration show that the DOAS is capable of accurately measuring SO2 with an error of 6%.
Notes: To evaluate the performance of the DOAS, the standard SO2 gas with a concentration of 100 ppm ±2% (supplied by Messer Co., Ltd-Ha) was introduced into the chamber. The gas flow rate is kept constant at 3 L/min to maintain the gas concentration at 100 ppm. The spectral characteristics of the Ce:LiCAF laser when passing through the air chamber will be recorded by the spectrometer two times.
The first time, the air chamber does not contain SO2 gas. The second time, the air chamber is filled with SO2 gas, then the laser beam will be partially absorbed by SO2 gas. The laser spectrum characteristics of the two recordings are shown in Figure 5.

## Slide 49
FLUORESCENCE IMAGE FROM THE SEED BEAM AXIS
Pump beam 1, 3
Pump beam 2, 4
Ce:LiCAF
Upper part pumping
Lower part pumping
Upper and lower part pumping

## Slide 50
The 9th Academic Conference on Natural Science for Young Scientists, Master and PhD Students from ASEAN countries (CASEAN-9)

## Slide 51
Time-resolved FLS1000
Photoluminescence Spectrometer
- Diode lamp: 250-325 nm (picosecond pulse: 100 ps)
- Laser diode: 375, 405 nm (picosecond pulse: 100 ps)
- Supercontinium fiber laser from 390 nm (femto second pulse ~ 100 fs)
- Flash lamp for phosphoresce (micro second)
Dr. Piyachat Meejitpaisan

## Slide 53
Fluorescence Lifetime Imaging Microscopy

## Slide 54: CONCLUSION
Ultrawide -band ultraviolet laser using Cerium-doped fluoride crystal was investigated theoretically and experimentally.
The DOAS system using the ultraviolet laser for determining SO2 gas concentration in the atmosphere has been developed. The results show that the DOAS system accurately determines the gas concentration with a measurement error of 6%.
These research findings open many potential applications for ultrawide-band ultraviolet lasers for environmental research.

## Slide 55
THANK YOU FOR
YOUR ATTENTION