Development of an Upgraded NaI(Tl) Crystal Encapsulation for the COSINE-100U Experiment: Maximizing Light Yield for Low-Mass Dark Matter Searches

In Soo Lee*1, Doohyeok Lee2, Jae Young Cho2, Chang Hyon Ha3, Eunju Jeon1, Hongjoo Kim2, Jinyoung Kim3, Kyungwon Kim1, SungHyun Kim1, Sun Kee Kim4, Won Kyung Kim5, Yeongduk Kim3,5, Young Ju Ko6, Hyunseok Lee5, Hyun Su Lee1,5, Jaison Lee1, Seo Hyun Lee5, Seung Mok Lee7, Reina H. Maruyama8, Jong-Chul Park9, Kangsoon Park10, Kihong Park1, Se Dong Park2, Kyungmin Seo1, Min Ki Son9& GyunHo Yu1

1Center for Underground physics, Institute for Basic Science, Daejeon, Korea.

2Department of Physics, Kyungpook National University, Daegu, Republic of Korea.

3Department of Physics, Chung-Ang University, Seoul, Republic of Korea.

4Department of Physics, Seoul National University, Seoul, Republic of Korea.

5IBS School, University of Science and Technology, Daejeon, Republic of Korea.

6Department of Physics, Jeju National University, Jeju, Republic of Korea.

7 Physics Department, Carnegie Mellon University, Pittsburgh, PA, USA

8Department of Physics and Wright Laboratory, Yale University, New Haven, CT, USA.

9Department of Physics and IQS, Chungnam National University, Daejeon, Republic of Korea.

10Yemilab Operation Center, Institute for Basic Science, Gangwon-do 26141, Republic of Korea.

islee@ibs.re.kr

The COSINE-100 experiment was designed to test the DAMA/LIBRA annual modulation claim using low-background NaI(Tl) detectors[1]. For the COSINE-100U upgrade, we have developed an advanced crystal encapsulation to enhance sensitivity to low-mass dark matter by significantly improving light collection efficiency and detector stability[2].

The upgraded design eliminates quartz optical windows, reducing optical interfaces by directly coupling photomultiplier tubes (PMTs) to the crystal surfaces using thin silicone optical pads[3]. For larger crystals, we introduced beveled crystal edges to efficiently guide scintillation light to 3-inch high-quantum efficiency PMTs. This configuration achieves a substantial performance gain, increasing the light yield by approximately 35–50% compared to the original COSINE-100 setup, with values exceeding 20 PE/keV at room temperature[2].

COSINE-100U has been operated at room temperature for an initial three-month period before transitioning to a cooled environment at -30°C. At this lower operating temperature, we observe a further increase in the intrinsic light yield, significantly lowering detector energy threshold[4]. Dedicated validation studies demonstrate that the encapsulation remains mechanically robust and optically stable during long-term operation in liquid scintillator at these temperatures[5].

In this talk, we present the encapsulation design details, the expected performance gains from the temperature transition, and the successful recovery of previously excluded crystals for high-sensitivity physics analysis at the new Yemilab facility.

1. COSINE-100 Collaboration, Model-independent search for annual modulation in COSINE-100, Phys. Rev. Lett. 123, 031302 (2019).

2 D. Lee et al., Upgrading the COSINE-100 experiment for enhanced sensitivity to low-mass dark matter detection, Commun. Phys. 8, 135 (2025).

3 NEON Collaboration, Upgrade of the NaI(Tl) crystal encapsulation for the NEON experiment, JINST 19, P10020 (2022).

4 K. Park et al., Validation of the COSINE-100U NaI(Tl) encapsulation for low-temperature operation in liquid scintillator, arXiv:2601.12819.

5 S.H. Lee et al., Study on NaI(Tl) crystal at −35°C for dark matter detection, Astroparticle Physics 141 102709 (2022).