## Slide 1
Development of cesium lead halide nanocomposite scintillators for high energy physics
Jan Král1,2, Vojtěch Zabloudil1,3, Vladimír Mašek1, Petr Liška4,5, Solangel Rojas1, Vladimir Babin2, Jan Valenta6, Václav Čuba1, Eva Mihóková1,2, Kateřina Děcká1,2, Etiennette Auffray3
SCINT 2026, Gyeongju, Korea, 28.5.2026
1 Faculty of Nuclear Sciences and Physical Engineering, Czech Technical University in Prague, Prague, Czech Republic
2 Institute of Physics of the Czech Academy of Sciences, Prague, Czech Republic
3European Organization for Nuclear Research (CERN), Meyrin, Switzerland
4 CEITEC, Brno University of Technology, Brno, Czech Republic
5 Institute of Physical Engineering, Faculty of Mechanical Engineering, Brno University of Technology, Brno, Czech Republic
6 Faculty of Mathematics and Physics, Charles University, Prague, Czech Republic

## Slide 2: Cesium lead halide nanocrystals
ABX3 (A=Cs+, MA+; B=Pb2+ ; X=Cl-, Br-, I-)
2
narrow tunable emission peak
Nano Lett. 2015, 15, 6, 3692–3696
excitonic ultrafast luminescence
K. Děcká, et al. Nanomaterials 2022, 12, 14.
  Time-of-Flight PET
coincidence time resolution
rise time
decay time
photon density
  Chromatic calorimetry
Notes: Dát obrázek toho calolimetru a heterostruktury

## Slide 3: Embedding nanocrystals into a polymer matrix
moving from bare nanocrystals or colloidal solutions to solid nanocomposite scintillators
3
polystyrene (PS)
polyurethane (PU)
epoxy resin (ER)
polydimethylsiloxane (PDMS)
poly(methyl methacrylate) (PMMA)
polyvinyl toluene (PVT)
tailoring nanocomposites for various application requirements
exploration of radiation hardness study of different nanocomposite
embedding procedure

## Slide 4: Embedding nanocrystals into a polymer matrix
moving from bare nanocrystals or colloidal solutions to solid nanocomposite scintillators
3
polystyrene (PS)
polyurethane (PU)
epoxy resin (ER)
polydimethylsiloxane (PDMS)
poly(methyl methacrylate) (PMMA)
polyvinyl toluene (PVT)
tailoring nanocomposites for various application requirements
exploration of radiation hardness study of different nanocomposite
Challenges:
suppression of thermal damage due to ligand desorption
protection from more polar polymer precursors
perform functionalization for copolymerization
embedding procedure

## Slide 5
Embedding nanocrystals into a matrix
4
nanocrystal synthesis
nanocrystal surface modification
ligand exchange

## Slide 6
Nanocrystal surface modification
4
nanocrystal surface modification
ligand exchange
nanocrystal synthesis
  ammonium hexaflurosilicate (AHFS)
platform for further functionalization by organosilanes to tune the nanocrystals for various matrices
fluoride surface treatment
formation of Si-O-Si network
CsPbBr3
CsPbBr3
talk on Limiting exciton diffusion enhances the photoluminescence of CsPbBr₃ nanocrystal films at high excitation densities by Simon Jessen (Aarhus University)
Thursday 28.5.2026 at 16:10
Challenges:
suppression of thermal damage due to ligand desorption
protection from more polar polymer precursors
perform functionalization for copolymerization

## Slide 7
Nanocrystal surface modification
5
nanocrystal surface modification
ligand exchange
nanocrystal synthesis
Challenges:
suppression of thermal damage due to ligand desorption
protection from more polar polymer precursors
perform functionalization for copolymerization

## Slide 8
Nanocrystal spectral tuning
6
nanocrystal surface modification
AHFS ligand exchange
nanocrystal synthesis
anion exchange
CsPbBr3 = CPB
CsPb(Br1-xClx)3 = CPBC
CsPbCl3 = CPC
org. Cd2+
org. Cd2+
spectral emission tuning
org. Cd2+ treatment for CPC and CPBC PLQY enhancement

## Slide 9
Embedding nanocrystals into a matrix
7
nanocrystal surface modification
AHFS ligand exchange
nanocrystal synthesis
thermal embedding procedure
embedding procedure
RT embedding procedure

## Slide 10: AHFS +ATMOS functionalization
8
AHFS + ATMOS = AA samples
AHFS = A samples
95% PLQY
60% PLQY
45% PLQY
Decreasing NC cluster size
transparency improvement with allyl-functionalization
reduced agglomeration
Jan Král et al. 2025 J. Phys. Mater. 8 015007

## Slide 11: PL and RL properties
9
PL and RL spectra preservation across range of NC loading and with polymerization temperatures up to 110°C
nanocrystal loading pushed up to 40 wt%
J. Mater. Chem. C, 2026,14, 4440-4450

## Slide 12: RL decay kinetics
ultra-fast multi-excitonic decay preserved to high loadings
significant acceleration of kinetics with chloride content
9

## Slide 13
(3-Aminopropyl)triethoxysilane
CPB@SiO2 polyurethane nanocomposites
Adapting the procedure for compatibilization with different polymer matrices
(3-Aminopropyl)triethoxysilane
for polyurethane matrix
  SiO2 shell for protection
  APTES for amino-functionalization
preserved PL/RL emission position
10

## Slide 14
11
Sample fabrication scaled to large volumes
and tailored for various matrices
CPX3 nanocomposites in various matrices
PDMS nanocomposites
polyurethane nanocomposites
subjected to radiation hardness study:
talk on Radiation stability of plastic and nanocomposite scintillators by Václav Čuba (CTU)
Monday 25.5.2026 at 11:54
epoxy nanocomposites
polystyrene nanocomposites
allyl-functionalization
SiO2 encapsulation
SiO2 encapsulation
amino-functionalization
+

## Slide 15
12
Samples for Chromatic calorimetry
scintillation prototype
August 2025 test beam at SPS facility
talk on Towards chromatic calorimetry using nanocomposite scintillators by Vojtěch Zabloudil (CERN, CTU)
Monday 25.5.2026 at 9:57
polystyrene nanocomposites
3×2×2 cm3 samples for chromatic calorimetry experiments

## Slide 16
13
3×2×2 cm3 samples for chromatic calorimetry experiments
Samples for Chromatic calorimetry
scintillation prototype
September 2025 test beam at CERN SPS facility
wavelength-shifting prototype
April 2026 test beam at CERN SPS facility
polystyrene nanocomposites
PDMS nanocomposites
WLS layers with superior optical coupling

## Slide 17
Conclusions and summary
developed AHFS functionalization enabling tailoring the NC surface for various polymer matrices
enhanced thermal polymerization resistance for bright CsPbBr3 polystyrene nanocomposite fabrication
improved transparency thanks to copolymerizable groups
radiation hardness under high-energy electron and proton radiation of various nanocomposites explored
CPX3 nanocomposites scaled and measured during test beam in CERN in chromatic calorimetry concept
14

## Slide 18
Acknowledgements
This work was carried out in the frame of the Crystal Clear Collaboration.
Supervisor: Etiennette Auffray (CERN)
Supervisor-specialists: Eva Mihóková (FZU) and Kateřina Děcká (CTU)
Collaborators: Ildefonso León Monzón (UAS), František Hájek (FZU), Michal Horák (CEITEC), Yacine Haddad (CERN), Anne-Mazarine Lyon (CERN), Matteo Salomoni (CERN), Michal Horák (CEITEC), Jean-Louis Faure (CERN)
15
The project received support from EIC pathfinder UNICORN project (GA 101098649).