Fabrication and properties of Tb-doped gadolinium oxysulfide scintillation ceramics for neutron imaging

Jiang Li1,2, Junlin Wu1,2, Dong Huang1,2, Chen Hu1,2, Jianrong Zhou3, Zhijia Sun3, Dariusz Hreniak4,

1State Key Laboratory of High Performance Ceramics, Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai 201899, China

2Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

3Spallation Neutron Source Science Center, Dongguan 523803, Guangdong, China

4Institute of Low Temperature and Structure Research, Polish Academy of Sciences, Okólna 2, 50-422 Wroclaw, Poland

Corresponding Author Email: lijiang@mail.sic.ac.cn

This is Neutron imaging in ray non-destructive detection has been widely studied due to its great application advantages. Terbium-doped gadolinium oxysulfide (Gd2O2S:Tb) scintillation powders have excellent application prospects in neutron imaging due to its high neutron absorption cross-section, high X-ray blocking ability, high light output and good physicochemical stability. The Gd2O2S powder scintillation screens prepared by Paul Scherr Institute (PSI) in Switzerland have shown very high application performance.

Neutron signal charge spectrum (the left) and Neutron spatial resolution (the right) of Gd2O2S:Tb ceramics.

In this work, the Gd2O2S:Tb powders with smaller lamellar particle size and more uniform dispersion were obtained by the hot water-bath method h.  Gd2O2S:Tb ceramics with the highest total optical transmittance of 20.3% at 545 nm and highest X-ray excited luminescence (XEL) intensity were obtained by hot pressing and HIP post-treatment. The XEL intensity of Gd2O2S:Tb ceramics is highest when the air-annealing temperature is 900oC, which is 1.3 times of that before annealing, and its neutron light output is 264 ph/n. The spatial resolution of neutron imaging of Gd2O2S:Tb ceramics (30 μm in thickness) is 17 μm, which is better than that of the Gd2O2S:Tb powder screen (20 μm) from PSI.

1. Junlin Wu, Jiyang Ding, Xinyou Huang, et al. Fabrication and microstructure of Gd2O2S:Tb scintillation ceramics from water-bath synthesized nano-powders: The influence of H2SO4 to Gd2O3 mole ratio. J. Inorg. Mater., 2023, 38(4): 452-460.

2. Junlin Wu, Dong Huang, Chen Hu, et al. Influence of LiF contents on the microstructure and optical properties of Gd2O2S:Tb scintillation ceramics. Opt. Mater., 2025, 168: 117439

Acknowledgments should appear near the bottom of the page.

This work was supported by the National Science and Technology Major Project (Grant No. 2024ZD0605900).