Growth and Characterization of  Radioactive source doped CeBr₃ Crystal Scintillators

Nguyen Thanh Luan1, H. J. Kim1,2*, J. Kaewkhao3,**, N. Singkiburin3, Gul Rooh1, Dong Woo Jeong2,

Joo Young Lee1, Nguyen Duc Ton2, M. H. Lee4,  E. K. Lee4, J. H. So4, Aagrah Agnihotri5, Jouni Suhonen5, Ioannis Gkialas6, S. Kothan7

1Center for High Energy Physics, Kyungpook National University, Daegu, Korea

2Department of Physics, Kyungpook National University, Daegu, Korea

3Center of Excellence in Glass Technology and Materials Science, Nakhon Pathom Rajabhat University, Nakhon Pathom, Thailand

4Center for Underground Physics, Institute for Basic Science, Daejeon, Korea

5Department of Physics, University of Jyväskylä, Jyväskylä, Finland

6University of the Aegean, Greece

7Department of Radiologic Technology, Chiang Mai University, Chiang Mai, Thailand

*Email: hongjoo@knu.ac.kr

** Email: jakrapong@webmail.npru.ac.th

Cerium bromide (CeBr₃) crystal scintillators have attracted significant attention for γ-ray spectroscopy due to their excellent scintillation performance such as a high light yield of approximately 60,000 photons/MeV, a fast decay time of about 20 ns, and an emission peak around 380 nm.  Owing to its low intrinsic background, in contrast to LaBr₃:Ce scintillators containing radioactive ¹³⁸La, CeBr₃ is particularly suitable for gamma-ray spectroscopy in space missions and rare nuclear process experiment. The source as a detector technique offers a novel approach to radiation detection by embedding a radioactive source within the scintillator, enabling self-detection, self-calibration, and enhanced signal detection efficiency [1,2]. This method eliminates the need for external detectors, improves sensitivity in low-background environments. The radioactive source doped CeBr₃ crystal scintillators were developed for the Global Rare Anomalous Nuclear Decay Experiment (GRANDE) [3]. We will present the growth and scintillation performance of intrinsic CeBr₃ and CeBr₃ crystals doped with three radioactive isotopes, 139Ce, 57Co and 44Ti. The CeBr3 powder was loaded into a quartz ampoule coated with radioactive isotopes under a nitrogen (N2) environment. The powder was dried at 110–150°C under a 10−7 torr vacuum for 12 hours and then torch-sealed for growth.  Special care should be taken for the preparation of radioactive source in the quartz ampoule for the successful growth of the radioactive source doped CeBr₃ crystal. Crystal was grown using the two zone Bridgman technique with a monitoring window. The growth rate was carefully controlled to maintain a stable interface, with a temperature gradient of 10–20°C/cm. The as-grown crystal was cooled to room temperature over three days.  Major scintillation characteristic including light yield, energy resolution, decay time, and non-proportionality of grown crystals are measured and compared.

References

[1] M. J. Kim, H. J. Kim, H. Park, K. Tanida , S. Kim, J. K. Cheon, K.B. Lee “Scintillation Properties of CsI:Na, 133Ba Crystal”, IEEE TNS Vol 60, No 2, 2013.

[2] D. H. Lee, E.J. Choi, H.S. Lee, N.T. Luan, J.H. So, H. J. Kim “Measurement of new 228Ac Isomers using a 228Ra doped CeBr3 scintillation crystal”, Radiation Physics and Chemistry 238 (2026) 113148

[3] A. Anihotri, J. Suhonen, H.J. Kim, “Constraints for rare electron-capture decays mimicking detection of dark-matter particles in nuclear transitions”, Physical Review Letters 1333 (2024) 232501.