Scintillation Properties of a Stilbene Crystal for Low-mass Dark Matter Search

Se Hwan Lee*1, Hongjoo Kim2, In Soo Lee*3 Young Ju Ko1, Jungho So4

1Department of Physics, Jeju National University, Jeju, Republic of Korea.

2Department of Physics, Kyungpook National University, Daegu, Republic of Korea.

3Center for Underground physics, Institute for Basic Science, Daejeon, Korea.

4Yemilab Operation Center, Institute for Basic Science, Gangwon-do 26141, Republic of Korea.

islee@ibs.re.kr

yjkophys@jejunu.ac.kr

The search for low-mass WIMPs is strongly motivated by the need to detect low-energy nuclear recoils, where target materials containing hydrogen provide a distinct advantage. Elastic scattering of low-mass WIMPs off hydrogen nuclei offers favorable kinematics, resulting in higher observable recoil energies compared to heavier target nuclei and thereby improving detection sensitivity at low thresholds[1]. Stilbene, an organic molecular crystal rich in hydrogen, naturally exploits this advantage while providing efficient scintillation response[2]. Furthermore, stilbene exhibits an anisotropic scintillation behavior in which the effective quenching factor depends on the recoil direction relative to the crystallographic axes, offering sensitivity to directional signatures of WIMP-induced nuclear recoils[3,4].

In this work, we measure the scintillation decay characteristics and effective light yield of a trans-stilbene crystal to evaluate its suitability for dark matter detection. The detector consists of a cylindrical stilbene crystal with a radius of 1 cm and a length of 1 cm, directly coupled to two photomultiplier tubes (Hamamatsu R12669) at both ends to maximize light collection efficiency. The scintillation waveforms are analyzed using a triple-exponential decay model, yielding decay time constants of approximately 8.7 ± 0.2 ns (fast), 20.0 ± 0.3 ns (medium), and 73.4 ± 1.5 ns (slow). Using a 241Am calibration source, the effective light yield is determined to be 3.2±0.1 photoelectrons per keV. In addition, pulse shape discrimination performance for gamma-ray and neutron events is studied using a 252Cf neutron source.

In this talk, we present the detector design, detailed scintillation property measurements, and PSD performance of the stilbene crystal, and discuss its potential as a next-generation scintillator for rare-event and dark matter searches.

[1] Lippincott, et al. HydroX, a light dark matter search with hydrogen-doped liquid xenon time projection chambers. Commun Phys 8, 244 (2025).

[2] Natalia Zaitseva, Andrew Glenn, Leslie Carman, H. Paul Martinez, Robert Hatarik, Helmut Klapper, Stephen Payne, Scintillation properties of solution-grown trans-stilbene single crystals, Nucl. Instrum. Methods A 789 (2015) 8-15

[3] Y Shimizu, M Minowa, H Sekiya, Y Inoue, Directional scintillation detector for the detection of the wind of WIMPs, Nucl. Instrum. Methods A 496 (2003) 347–352

[4] R.A. Weldon, J.M. Mueller, J. Mattingly, Exploiting stilbene’s scintillation anisotropy for neutron source localization, Nucl. Instrum. Methods A 967 (2020) 163834