Thallium-based new high-density scintillator crystal: Tl2SiF6

D. Joseph Daniel1, Sunghwan Kim2, and H. J. Kim1,*

1The Center for High Energy Physics, Kyungpook National University, Daegu 41566, Republic of Korea

2Department of Radiological Science, Cheongju University, Cheongju, 28503, South Korea

*Corresponding Author Email: hongjoo@knu.ac.kr

Figure 1. Digital photograph of a grown scintillator single crystal: Tl2SiF6

Heavy metal ions with an ns² electronic configuration typically give rise to pronounced luminescence under ambient conditions due to their favorable electronic transitions [1]. Consequently, thallium-based scintillator crystals have attracted growing interest, as their high density and large effective atomic number enable efficient absorption of high-energy X-rays and γ-rays, making them promising candidates for radiation detection applications [2]. In this present investigation, for the first time, we report that the scintillation properties of Dithallium hexafluorosilicate (Tl2SiF6) crystal scintillator. The single crystals were grown using the solvothermal method. Fig. 1 presents a digital photograph of the grown single crystal. In contrast to previously reported thallium-based halide scintillators that exhibit hygroscopic behavior, the grown crystals are non-hygroscopic and stable under ambient conditions. Structural analysis reveals that the grown crystal Tl2SiF6 crystallizes in the cubic crystal system with the space group Fm3m. Under X-ray excitation, the Tl2SiF6 crystal exhibits a strong intrinsic emission band maximum at 298 nm. The scintillation decay measurements performed under γ-ray excitation from a ¹³⁷Cs source reveal a dominant decay component of 228 ns, contributing approximately 94% of the total emission intensity. Further investigations of the scintillation response and other relevant material properties will be discussed in detail.

References:

- A. Vogler and H. Nikol , The structures of s2 metal complexes in the ground and sp excited states. Comments Inorg. Chem., 1993, 14 , 245 – 261.

- HongJoo Kim et al., Thallium-based heavy inorganic scintillators: recent developments and future perspectives. : CrystEngComm, 2022, 24, 450.