Bridgman growth and luminescence properties of Na-doped Li2MoO4 crystals

Aoqi Xu1, Liang Chen1, Wei Xiong1, Yao Zhou1, Hui Yuan1

1National Key Laboratory of Functional Crystals and Devices, Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai 20050, China

Corresponding Author Email: hyuan@mail.sic.ac.cn

Na-doped Li2MoO4 crystals were grown using the Bridgman method with Na2Mo2O7, Na2CO3, and Na2MoO4 as dopants. X-ray diffraction and Raman spectroscopy confirmed that Na2Mo2O7 doping preserves the host structure of Li2MoO4, while modifying the MoO42- group vibrational modes and crystal field environment through the introduction of Mo2O72- units. Fluorescence studies revealed modest luminescence enhancements (1.3 times and 1.6 times relative to pure Li2MoO4) for samples doped with 1 mol% Na2CO3 and 0.8 mol% Na2MoO4. In contrast, Na2Mo2O7 doping significantly outperformed these, with an optimal concentration of 0.8 mol% yielding a 9 times increase in luminescence intensity. This substantial enhancement underscores the dominant role of Mo2O72- groups, rather than Na+ ions, in enhancing luminescence. The Na2Mo2O7-doped crystals display temperature-dependent luminescence behavior similar to pure Li2MoO4, with emission intensity increasing markedly as temperature decreases.

Key words: Li2MoO4 crystal, Doping, Bridgman method, Luminescence.