Features of Czochralski growth of 2-inch Ce-doped Y-Al-Ga garnet crystals for scintillator applications

Yasuhiro Shoji1, Kei Kamada1,3, Vladimir Kochurikhin1, Liudmila Gushchina1, Hisato Suezumi2, Masao Yoshino1,2, Akira Yoshikawa1,2,3

1C&A corporation, Sendai, Japan

2Institute for Materials Research, Tohoku University, Sendai, Japan

3New Industry Creation Hatchery Center, Tohoku University, Sendai, Japan

Corresponding Author Email: y_shoji@c-and-a.jp

Recently, Ce-doped Gd-Al-Ga garnet single crystal (GAGG) have emerged as a promising scintillator material due to its high light yield (up to 53,000 photons/MeV) and fast decay times (76 and 794 ns). The growth technology for this crystal has been well developed, and boules up to 4 inches in diameter have been successfully grown [1].

Ce-doped Y-Al-Ga garnet (YAGG) is another prospective scintillator material mainly due to its shorter decay time in comparison with GAGG (20-40 ns). 1-inch YAGG crystals were successfully grown using the Czochralski technique [2].

GAGG and YAGG 2-inch crystals grown under the same conditions

However, our attempts to grow 2-inch YAGG crystals under the same conditions used for GAGG resulted in a significant deterioration in crystal quality. The melting temperature of YAGG is approximately 100 °C higher, leading to intense Ga₂O₃ evaporation during growth and a highly nonuniform composition along the length of the crystal. In addition, the irreversible loss of iridium (the crucible material) during a single YAGG growth cycle reached 6.2%, significantly increasing production costs. Moreover, small iridium particles floating on the melt surface caused substantial distortion of the cylindrical shape of the crystal.

Careful optimization of the growth conditions—including the ceramic hot-zone structure, growth parameters, melt composition, and growth atmosphere—resulted in a significant improvement in the quality of the grown 2-inch YAGG crystals. In particular, replacing the conventional N₂ + CO₂ growth atmosphere used for large GAGG crystals with Ar + O₂ reduced iridium loss to 1.6%. Careful selection of the hot-zone configuration also helped to prevent crack formation in the crystals.

In this report, we compare the optical and scintillation properties of 2-inch YAGG crystals grown under different conditions with those of commercially available large GAGG crystals.

- V. Kochurikhin et al. “Czochralski growth of 4-inch diameter Ce: Gd3Al2Ga3O12 single crystals for scintillator applications”, J. of Crystal Growth 531, 125384 (2020)

- O. Sidletskiy et al. “Structure and scintillation yield of Ce-doped Al-Ga substituted yttrium garnet”, Materials Research Bulletin, 47, 3249-3252 (2012)