## Slide 1
Notes: First, I like to thank the organizers, in particular Hong-Joo Kim, and the International Advisory Committee for inviting me to deliver this opening lecture for this conference. I feel honored. On Thursday before the banquet we have a brainstorming on the future of scintillation research, and I felt that in order to discuss about the future one should know about the past. This explains the title of my presentation The history of scintillation discovery and the challenges that lie ahead. I will also go into the history of our community.

## Slide 2: Outline
History of scintillator discovery
  Tl activated scintillators
  BGO, BaF2, LSO, garnets
  Ce3+ activated scintillators
Enablers and drivers of discovery and development
  Technological enablers
    PMT, PD, Si-PM
    Availability of purified rare earths
  User demands (HEP, medical diagnostics, safeguarding)
  Fundamental knowledge, new theory, curiosity
Challenges that lie ahead
Notes: What I want to do is to walk you through the history of scintillator discovery. When was what invented and why? What were the drivers of a discovery.
Along my presentation I will show pictures of key players in scintillation research. Many are still around here at this conference. I will show photo’s at an age when they made their discovery or when they provided their important contribution. You may reckognize yourself or your colleague

## Slide 3
Discovery of NaI:Tl in 1948
Notes: Weber distinguished 3 phases in scintillator discovery. 1) visual scintillation counting discovery of radioactivity, X-rays, alpha particles. 2) after invention/availability of the PMT 1946-1980. During this phase BGO was discovered

## Slide 4
NaI:Tl and CsI:Tl

## Slide 5
Enabler: availability of PMTs after WWII
Driver: the need to detect the elusive gamma rays
First pulse height spectrum in 1950
Notes: Weber distinguished 3 phases in scintillator discovery. 1) visual scintillation counting discovery of radioactivity, X-rays, alpha particles. 2) after invention/availability of the PMT 1946-1980. During this phase BGO was discovered

## Slide 6
Enabler: chemical purification of the rare earths in the 1960ties
Discovery of Y3Al5O12:Ce by G. Blasse in 1967
Notes: YAG;Ce represents an entire class of materials. The garnets. Many variants are important as scintillator.

## Slide 7
Knowledge from inspiring scientists in phosphor research as an enabler and driver of scintillator development
patented by company Philips in 1974 as phosphor for tube lighting
Notes: In 1967 Blasse still a young scientist. 20 years later when I entered the field he inspired me a lot. I collected all his published papers.

## Slide 8
Y3Al5O12

## Slide 9
Discovery of Bi4Ge3O12 (BGO) 1973-1975
Notes: Weber distinguished 3 phases in scintillator discovery. 1) visual scintillation counting discovery of radioactivity, X-rays, alpha particles. 2) after invention/availability of the PMT 1946-1980. During this phase BGO was discovered

## Slide 10
Notes: Weber realized the potential as scintillator

## Slide 11
The pulse height spectrum is the birth certificate of a new scintillator

## Slide 12
Medical diagnostics and high energy physics were the drivers for the further development of BGO
BGO became standard scintillator for most commercial PET scanners in 1980s-1990s
User demands (medical diagnostics) as a driver of scintillator development
Notes: Cho and Farukhi realized potential application
Discovery is one thing, development is another

## Slide 13
CsI calorimeter for CLEOII detector at Cornell University 1989
User demands (HEP) as a driver of scintillator development
BGO calorimeter for L3 at CERN 1989 using 12 tons of BGO (SIC)
Notes: BGO became also the crystal of choice for the L3 experiment at CERN

## Slide 14
First the slow component and couple of years later the fast component
Discovery of the fast component in BaF2 (1982)

## Slide 15: Discovery fast component in BaF2 in 1982
BaF2 - fast UV luminescence
First observation of fast 220nm component (decay time <10ns)
Residual impurities were suggested to be responsible
Notes: The fast component is at 220nm in the UV and you need UV sensitive PMTs hence it later discovery then the slow component

## Slide 16
Medical imaging as driver of BaF2 development
High energy Physics as driver of BaF2 development
BaF2 for the detector system TAPS
Notes: At this time, I entered as a young scientist in the field of scintillation research in the group of Carel van Eijk. Paul Schotanus was stil around as a postdoc and taught me the tricks of scintillators characterization.
Now CEO of his company Scionix in The Netherlands

## Slide 17: Explanation fast component in BaF2 in 1984
Excitation onset at 18 eV
Evidence of core-valence emission
Decay time <7ns
Notes: The fast component is at 220nm in the UV and you need UV sensitive PMTs hence it later discovery then the slow component

## Slide 18: Measuring fast component in BaF2 (1986)
BaF2 - fast UV luminescence
Notes: Verify if this is indeed Kubota

## Slide 19
Speed is important
Ce3+ 5d-4f emission is fast (17-60 ns)
The Ce3+ doped scintillators
Notes: Weber distinguished 3 phases in scintillator discovery. 1) visual scintillation counting discovery of radioactivity, X-rays, alpha particles. 2) after invention/availability of the PMT 1946-1980. During this phase BGO was discovered

## Slide 20
The discovery of Lu2SiO5:Ce3+ in 1992
Oil-well logging as driver for LSO discovery and development
Notes: Yiu see that LSO is much faster than NaI:Tl and BGO. Eventually it replaced BGO in PET-scanners.

## Slide 21
Strong afterglow with more than 1 hour 1/e decay time at room temperature
Notes: I will come back on the afterglow problem later

## Slide 22
Crystal2000 Chamonix, France, September 22-26, 1992
The SCINT conference series as drivers of scintillating material discovery
Paul Lecoq
PbWO4 calorimeter for CMS at CERN
Notes: In the meantime the first scintillator conference was organized by Paul Lecoq, the founding father of this conference series that bring us here together today.

## Slide 23
1992
1994
1995

## Slide 24
Scintillator studies/development at TU-Delft 1988-2005
Lu2SiO5:Ce (LSO)
K2LaCl5:Ce (first Ce doped halide)
Cs2LiYCl6:Ce (CLYC neutron scintillator)
LuCl3:Ce
LuBr3:Ce
LaCl3:Ce3+
LaBr3:Ce3+
Notes: LSO:Ce was already mentioned. We performed studies in collaboration with Charles Melcher.
Initially we started with BaF2 (together with Paul Schotanus). Suppression of slow component with la doping
Pr and Nd doping LuAG:Pr
Collaboration with Bern University and Saint-Gobain Research

## Slide 25
The discovery of LaCl3:Ce3+ in 2000
Now we knew we really had something very good!

## Slide 26
The discovery of LaBr3:Ce3+ in 2001
Now we knew we really had something even better!

## Slide 28
Karl Krämer, expert halide crystal grower, was an enabler of scintillator discovery in Delft

## Slide 29
Notes: 9-11 terrorist attack on twin towers became a driver scintillator discovery (in US). Ceramic Gd3Al3ga2O12:Ce and Cs2LiLaBr6:Ce are commercially available, but for the rest no new discoveries that led to a successful commercial product.

## Slide 30
Notes: We see that co-doping is a rising research trend

## Slide 31
How engineering and co-doping is driving scintillator development
Lu2SiO5:Ce3+ invented by Melcher and Schweitzer in 1992
High melting point 2700C lowered by 100C due to Y
economic issue, i.e., cost reduction, as a driver of innovation
Afterglow problem (not solved by Y-co-doping/solid-solution)
(Lu,Y)2SiO5:Ce3+ improvement patented by Bruce Chai et al. 2003
Notes: Bruce Chai generous sponsor of the Banquet of Scint conferences
President of Crystal Photonics

## Slide 32
oxygen vacancy electron traps
Notes: I will come back on the afterglow problem later

## Slide 33
1%Ca
0.5%Ca
First patented in 2005
Improving LSO:Ce by means Ca2+ of co-doping
Notes: The initial idea was that electron trapping in oxygen vacancies was responsible for the afterglow. The idea was by means of c-doping to alter oxygen defect structure.

## Slide 34
Ce3+ 4f-5d absorption bands
In the luminescence phosphors field, it was always believed that Ce4+ kills the Ce3+ emission

## Slide 35
Ce3+ + hole  Ce4+
Ce4+ + electron(Ce3+)*scintillation photon
Ce4+ + electron(Ce3+)*scintillation photon
Ce3+ + hole Ce4+
Strong afterglow reduction
Increase of light yield
Shorter rise time
  Better timing
VRBE scheme

## Slide 36
Ce3+ + hole  Ce4+
Ce4+ + electron(Ce3+)*scintillation photon
Ce4+ + electron(Ce3+)*scintillation photon
Ce3+ + hole Ce4+
Strong afterglow reduction
Increase of light yield
Shorter rise time
  Better timing
VRBE scheme

## Slide 37
Ce3+ + hole  Ce4+
Ce4+ + electron(Ce3+)*scintillation photon
Ce4+ + electron(Ce3+)*scintillation photon
Ce3+ + hole Ce4+
Strong afterglow reduction
Increase of light yield
Shorter rise time
  Better timing
VRBE scheme

## Slide 38
Mg2+ co-doping30% higher light yield and less slow component
Notes: Shanghai Institute of Ceramics in collaboration with Martin Nikl

## Slide 39
Engineering of the garnet phosphors and scintillators
P. Dorenbos
The color of 5d-4f emission can be tunedLED-phosphor
Temperature of thermal quenching can be optimized
Density by admixing Lu or Gd can be optimized
Optimization by co-dopants (like Mg2+)

## Slide 40: Scintillator non-proportional response to energetic electrons
Cherepy et al. IEEE Trans. Nucl. Sci. 56(3) (2009) 873
NaI:Tl. LSO:Ce
Strongly
Non-proportional
LaBr3:Ce
LaCl3:Ce
YAlO3:Ce
proportional
Notes: The light yield of a scintillator is expressed in photons/MeV. Ideally that number should be independent on the gamma ray energy. In that case we speak of a perfect proportional response. In the figure above the light yield is normalized to unity at 500 keV. For the ideal response one expects a constant. In reality, the response depends on the energy of the electron that creates the ionization track. LSO (Lu2SiO5) and NaI:Tl have a strong non-proportionality. LaBr3:Ce shgow must more constant response.

## Slide 41
Non-proportionality is not a given property
Notes: Non-proportionality is not an unchangeable property of scintillators. It depends on concentration and on temperature.

## Slide 42
LaBr3:Ce3+;50ppm Sr2+
Synchrotron X-ray energy
50 ppm of Sr2+ improves performance dramatically

## Slide 43: Challenges that lie ahead
It seems (to me) that traditional new scintillator discovery does not lead easily to new commercial products. It is hard to beat the existing products, and the traditional research fields have been largely explored.
By means of co-doping and/or engineering strategies, properties can still be improved
  Improving crystal growth properties LYSO
  Engineering the proportionality LaBr3:Ce 50ppm Sr2+
  Shortening the rise time LYSO:Ce;Ca
  Improving thermal stability
What I learned is that 0.1 eV change in electronic level locations (valence band, conduction band, luminescence center), may alter performance dramatically
Notes: Perhaps a theme at the brainstorming session of Thursday

## Slide 44
Should we explore entirely new research fields
  Direct bandgap emission (Pb-perovskite halides)
  Semi-conducting compounds
  Hybrid materials, nano materials, plastics
scintillation materials discovery by means of
  machine learning
  computational simulation
Challenges that lie ahead
But!
  50 ppm of co-dopant may improve scintillator performance strongly (we don’t know why)
  0.1 eV change in Ce3+ 5d-level relative to CB-bottom100K change in quenching temperature
My guess: for the time being at best one may predict what will not work but not what will work

## Slide 45: Challenges that lie ahead
if the arrival time of each individual photon from each scintillation event can be detected, almost full information can be used
Waveform digitizers, fast photon detectors and artifical intelligence for data management and analysis
Wolszczak NIM A886 (2018) 30
More information from the same data

## Slide 47: (BM)2PbBr4 and dielectric engineering BM=benzimidazole
Exciton binding energy enhanced to 360 meV by
confinement 3D2D
by a small dielectric constant of organic spacer layer
Decay time changes with 1/Eehreduced decay time
Mengling Xia et al. Adv. Mater. 35 (2023) 2211769
195 meV
360 meV

## Slide 48: (BM)2PbBr4 and dielectric engineering BM=benzimidazole
Mengling Xia et al. Adv. Mater. 35 (2023) 2211769
light yield of 3190 ph/MeV at 662 keV
decay of 0.97 ns

## Slide 49
Take away message
Usually, Ce3+ is a poor emitter or not at all on large La-sites
  e.g. La2O3, LaAlO3
  before 2000 we focused on Ce3+ doping on small Y or Lu sites
  however, LaCl3 and LaBr3 turned out to be the best
Usually, the presence of Ce4+ kills Ce3+ emission
  and always reducing synthesis conditions were applied
  however, Ce4+ due to Ca2+ or Mg2+ co-doping can improve scintillator performance
  only when the CT-absorption band at higher energy than 5d-4f emission band!
Take away message: do not mislead yourself by trends. Nature is much more versatile.

## Slide 50: Additional fast components in BaF2 (1985)
BaF2 - fast UV luminescence
195nm and 175nm band
Decay time <3ns
220nm
195nm
175nm