The development of new Ce3+ doped silicophosphate glass for X-ray scintillator and application to synchrotron x-ray imaging

E. Kaewnuam1, N. Wantana2,3,*, Y. Ruangtaweep2,3, F. Khrongchaiyaphum2, 3, N. Chanthima2, 3,  
M. Tungjai4, P. Pakawanit5, C. Phoovasawat5, J.Y. Cho6, H.J. Kim7, N. Intachai4, S. Kothan4, 
J. Kaewkhao2,3

1Faculty of Science and Technology, Muban Chombueng Rajabhat University, Ratchaburi, 70150,

Thailand

2Physics Program, Faculty of Science and Technology, Nakhon Pathom Rajabhat University, Nakhon Pathom, 73000, Thailand

3Center of Excellence in Glass Technology and Materials Science (CEGM), Nakhon   Pathom Rajabhat University, Nakhon Pathom, 73000, Thailand

4Center of Radiation Research and Medical Imaging, Department of Radiologic Technology, Faculty of Associated Medical Sciences, Chiang Mai University, Chiang Mai, 50200, Thailand

5Synchrotron Light Research Institute (Public Organization), Synchrotron Research and Applications Division, 111 University Avenue, Muang District, Nakhon Ratchasima 30000, Thailand

6The Center for High Energy Physics, Kyungpook National University, Daegu, 41566, Republic of Korea

7Department of Physics, Kyungpook National University, Daegu, 41566, Republic of Korea

Corresponding Author Email: wnuanthip@webmail.npru.ac.th

This work studied the effect of CeF3 concentration on P2O5-Gd2O3-ZnO-Al2O3-Na2CO3-SiO2-xCeF3 glass properties to develop as the scintillator for X-ray imaging.

Synchrotron x-ray imaging of Bloodberry captured by using SiPCe glass as scintillator compared to YAG:Ce crystal

The density and refractive index of glass increased by more doping CeF3 content. All glasses performed high transparency in visible light, while the absorption of Gd3+ and Ce3+ was obviously dominant in UV region on CeF3-undoped and CeF3-doped glasses respectively. Photoluminescence (PL) of glasses were investigated under direct Ce3+ excitation (ex = 305 nm) and Gd3+ - Ce3+ energy transfer process (ex = 275 nm). With direct Ce3+ excitation, glass exhibited the highest PL intensity of Ce3+ (5d  4f) around 330 - 345 nm. This generated blue light emitting and its decay time of Ce3+ were short around tens of nanosecond order. PL intensity and decay time at 311 nm of Gd3+ in glass decreased via CeF3 addition revealing the Gd3+  Ce3+ energy transfer. The photoluminescence quantum yield of 0.30 mol%-CeF3 doped glass with ex = 305 nm and 275 nm was 34.95 % and 20.23 % respectively. Under X-ray excitation, this glass sample performed the strong emission with radioluminescence (RL) light at 95% of BGO scintillator. The light yield of glass irradiated by -ray (0.662 MeV) from 137Cs source was around 220  22 ph/MeV. This developed glass was used as scintillator for capturing the object which its image quality was slightly less than image by commercial YAG:Ce crystal. It represented the high performance of glass scintillator for practical X-ray imaging operation.