Sm3+-doped Sodium Yttrium Borate Glass for X-ray Imaging Scintillator

N. Wantana1,2, E. Kaewnuam3,*, F. Khrongchaiyaphum1,2, Y. Ruangtaweep1,2, T. Keawmon1,2,

P. Pakawanit4, C. Phoovasawat4, N. Intachai5, S. Kothan5, H.J. Kim6 and J. Kaewkhao1,2

1Center of Excellence in Glass Technology and Materials Science (CEGM), Nakhon Pathom Rajabhat University, Nakhon Pathom, 73000, Thailand

2Physics Program, Faculty of Science and Technology, Nakhon Pathom Rajabhat University, Nakhon Pathom, 73000, Thailand

3Faculty of Science and Technology, Muban Chombueng Rajabhat University, Ratchaburi, 70150, Thailand

4Synchrotron Light Research Institute (Public Organization), Synchrotron Research and Applications Division, 111 University Avenue, Muang District, Nakhon Ratchasima, 30000, Thailand

5Center of Radiation Research and Medical Imaging, Department of Radiologic Technology, Faculty of Associated Medical Sciences, Chiang Mai University, Chiang Mai,

50200, Thailand

6Department of Physics, Kyungpook National University, Daegu, 41566, Republic of Korea

Corresponding Author Email: Eakgapon_9@hotmail.com and Eakgapon@mcru.ac.th

In this work, Sm3+-doped sodium yttrium borate glasses were studied and developed for X-ray detection. The influence of Sm2O3 concentration (0 - 2 mol%) on the glass physical, optical, and luminescence properties were investigated to find out the optimum glass composition.

3D-image of Sponge captured by X-ray imaging used 
1 mol%-Sm2O3 doped sodium yttrium borate glass as scintillator

The 4f-4f transition from 6H5/2 ground state of Sm3+ caused the glass’s absorption in visible light and near-infrared region which its absorption strength increased by following Sm2O3 content. Under excitation at 403 nm, glasses exhibited the strongest photoluminescence (PL) at 600 nm under Sm3+ transition from 4G5/2 luminescence level. The radioluminescence (RL) of glasses under X-ray excitation were investigated and their spectrum pattern were similar to those of PL. Glass doped with 1 mol%-Sm2O3 owned the highest emission intensity in both PL and RL spectra due to concentration quenching effect. Additionally, PL and X-ray scintillation decay time of glasses decreased in milliseconds range with added Sm2O3 concentration.

Finally, 1 mol% doped glass was used as scintillator for practical X-ray imaging, and it yielded the satisfied quality of image compared to YAG:Ce scintillator. This developed glass is a promising material for static X-ray imaging and orange photonic applications.